- Crossing Functional Boundaries: Multi-Physics Empowered Smart Structures

Modern civil engineering is undergoing a profound paradigm shift, transitioning from the design of purely load-bearing structural elements to the development of sophisticated, multi-physics empowered smart systems[1]. Traditional design philosophies have fundamentally isolated mechanical performance from other physical phenomena, limiting the adaptive capacity and operational scope of infrastructure in complex, dynamic environments[2, 3].

Metamaterials overcome these conventional boundaries by serving as intelligent carriers of multi-field coupling[4]. Through the precise engineering of their artificial microstructures, these advanced materials extend the role of structural components far beyond passive mechanical resistance, actively bridging multiple physical domains[5].

Specifically, the integration of multi-physics metamaterial concepts introduces transformative capabilities across several critical dimensions. By manipulating acoustic and elastic wave fields, these structures enable highly effective wave energy shielding, offering novel diversion-based pathways for seismic protection and noise attenuation[6, 7]. In the thermal domain, rationally designed microscopic anisotropy facilitates passive, zero-energy thermal regulation for smart building envelopes[8, 9]. Additionally, the embedding of electromagnetically responsive micro-architectures transforms standard construction materials into self-sensing composites, granting structures intrinsic health-monitoring and self-perception capabilities without vulnerable external wiring[10, 11]. Likewise, in the hydrodynamic domain, metamaterial arrays redirect and dissipate water waves, creating sheltered “quiet zones” around offshore installations and adaptive breakwaters that mitigate scour and impact loads. This section systematically reviews these cross-disciplinary advancements, highlighting how multi-physics integration is fundamentally redefining the operational boundaries of future civil infrastructure.

Fig. X Multi-physics empowered smart structures: a1, seismic cloaking foundations[12]. a2, acoustic metamaterials noise barriers[13]. a3, underwater acoustic wave attenuation[14]. b1, applications of transformation theory: cloaks, concentrators and rotators[9]. b2, schematic of a radiative cooling surface with four heat exchange processes[15]. b3, thermal diode with forward heat conduction and reverse thermal insulation[16]. c1, metastructure substrate piezoelectric energy harvester[17]. c2, mechanism and applications of electromagnetic wave absorbing cmentitious metamaterials[18]. c3, structural design of the metamaterial sensor[10]. d1, structures for water wave manipulation[19]. d2, schematic and simulated amplitude profiles of a water wave concentrator with baffles[20]. d3, schematic of the invisibility concentrator concept and simulated field patterns comparing an isolated large cylinder with the cylinder enclosed by the concentrator[20].

  - Acoustic/Elastic Wave Field: Local Noise Reduction and Global Cloaking

The manipulation of acoustic and elastic waves in civil infrastructure is fundamentally rooted in phononic crystal theory[21]. At the micro-structural level, the wave-attenuating capabilities of these metamaterials rely on two primary mechanisms: local resonance[22] and Bragg scattering bandgaps[23]. Local resonators utilize the resonance of internal mass-spring components to absorb and trap low-frequency wave energy at sub-wavelength scales. Conversely, Bragg scattering utilizes the periodic spatial arrangement of materials with contrasting elastic properties. This periodicity causes propagating waves to destructively interfere with one another, effectively creating structural bandgaps that strictly prohibit the transmission of waves within specific frequency ranges.

On a macroscopic scale, these micro-designs translate into paradigm-shifting protective systems. A prominent and highly researched application is the development of metamaterial seismic cloaking foundations. Traditional seismic engineering typically relies on structural mass, stiffness, or base isolation to “hard resist” or absorb earthquake energy. In contrast, seismic cloaks function by actively altering the propagation path of damaging surface Rayleigh waves, as illustrated in Fig. X a1. By carefully designing the effective refractive index of the soil-structure interface, these metamaterial arrays divert seismic waves around the protected structural zone, effectively guiding the energy away and leaving the internal infrastructure undisturbed.

Beyond seismic cloaking, acoustic metamaterials offer superior solutions for environmental and ecological noise mitigation. High-efficiency acoustic metamaterials noise barriers, as shown in Fig. X a2, are highly applicable for infrastructure plagued by severe, low-frequency traffic noise, such as highways, high-speed rail lines, and airports, where traditional concrete soundwalls often fail. Furthermore, the application of these principles extends to critical marine environments. During the construction of offshore wind farms, the deployment of underwater acoustic metamaterial barriers, as depicted in Fig. X a3, around piling sites can drastically attenuate high-intensity hydroacoustic shocks. This targeted frequency shielding is crucial for protecting vulnerable marine life from acoustic trauma, demonstrating the versatility of metamaterials in bridging structural engineering with ecological preservation.

  - Thermal Field: Passive Control and Zero-Carbon Buildings

Transformation thermotics exploits the form-invariance of the heat conduction equation to prescribe spatially inhomogeneous and highly anisotropic thermal conductivity tensors[24]. These are physically realized through graded composites, multilayer laminates, or architected cellular solids, enabling precise manipulation of heat flux along curvilinear paths[25]. The resulting phenomena include thermal cloaking that shields interior regions, thermal concentrating that intensifies flux, and even apparent negative thermal conductivity, where heat flows from cold to hot. Fig. X b1 illustrates these transformation-theory devices, including cloaks, concentrators, and rotators. This represents a paradigm shift from passive insulation to active, directional heat-flow control, establishing the foundational physics for intelligent building envelopes.

Translating this microscopic anisotropy into macroscopic thermoregulation, materials with strongly nonlinear, thermally responsive conductivity enable a “temperature trapping” mechanism. Above a designed critical temperature, the material abruptly switches to a low-conductivity state, suppressing heat ingress; below that threshold, it remains highly conductive, facilitating heat retention. This behavior corresponds to a thermal diode with forward conduction and reverse insulation[26], as depicted in Fig. X b3. Consequently, this homeostatic behaviour maintains a nearly constant interior temperature despite large ambient fluctuations, functioning as an energy-free, fully passive thermostat. The adaptive thermal rectification thereby achieved aligns passively with diurnal and seasonal climatic cycles.

In parallel, passive radiative cooling (PRC) is realized via ultra-broadband metamaterial surfaces. Architectures such as metal-dielectric-metal multilayers, hierarchically porous polymer coatings, and bioinspired honeycomb structures simultaneously achieve solar reflectance exceeding 97% and near-unity selective emissivity within the primary atmospheric transparency windows[15]. Fig. X b2 provides a schematic of a radiative cooling surface with its four key heat exchange processes. By coupling this tailored spectral response to the cold sink of deep space, these surfaces attain continuous sub-ambient temperatures even under direct solar illumination, effectively rejecting building heat without any mechanical work or refrigerant.

Bringing these concepts together at the system level results in a zero-carbon smart structural cladding. In summer, the outer PRC layer radiates excess heat to the sky, while internally graded thermal-metamaterial pathways, exploiting directional cloaking, divert incoming environmental heat flows around the occupied space. In winter, the temperature-trapping layer autonomously locks internal heat by switching to an insulating state whenever the interior rises above the comfort setpoint. This dual-mode, all-passive envelope simultaneously provides winter warmth and summer coolness without auxiliary energy, integrating radiative sky cooling, nonlinear thermotics, and engineered heat guiding into load-bearing façades. Such claddings thereby realize a zero-energy building environment, reducing carbon footprint through materials physics rather than energy-intensive HVAC systems.

  - Electromagnetic Field: Load-Bearing and Sensing Integration

Contemporary infrastructure is increasingly transcending passive paradigms by adopting multifunctional electromagnetic metamaterials, which now span energy harvesting, wave absorption, and structural sensing. At the microscopic level, this convergence is realized by embedding subwavelength resonant microstructures directly within cementitious matrices, without compromising load-bearing integrity[27-29].

One prominent application is the conversion of ambient mechanical vibrations into electrical energy. Fig. X c1 presents a metastructure substrate piezoelectric energy harvester, in which a structured metamaterial substrate amplifies local strain onto a piezoelectric element, efficiently scavenging energy to power wireless nodes. A second critical function is electromagnetic wave absorption. As illustrated in Fig. X c2, the mechanism and applications of absorbing cementitious metamaterials rely on impedance-matched resonators that dissipate incident microwave energy as heat, delivering broadband electromagnetic shielding while preserving mechanical performance.

Most crucially for structural health monitoring, these embedded resonators enable wireless, self-sensing functionality. Fig. X c3 shows the structural design of a metamaterial sensor, wherein localized geometric or dielectric perturbations shift the effective capacitance and inductance of the resonators. These alterations produce measurable frequency shifts in the macroscopic scattering parameters, observable as resonance-dip migrations in microwave reflection or transmission spectra. Remote, non-contact antennas can capture these spectral fingerprints without internal power or wired connections, realizing passive, real-time damage perception. The synthesis of subwavelength metamaterial design with applied electromagnetics thus integrates load-bearing, wave-absorbing, energy-harvesting, and self-sensing functionalities, paving the way for resilient, autonomous civil infrastructure.

  - Hydrodynamic Field: Ocean Wave 'Cloaking' and Fluid-Structure Interaction Control

In the hydrodynamic domain, structural metamaterials are fundamentally redefining fluid-structure interactions, evolving from passive physical barriers into intelligent mechanisms for advanced wave manipulation. The theoretical foundation of this capability is anchored in transformation hydrodynamics, which exploits the formal mathematical analogy between two-dimensional Maxwell’s equations and the linearized shallow-water wave equations[30, 31]. Because these governing equations maintain form invariance under coordinate transformations, wave propagation paths can be precisely controlled by spatially modulating the local equivalent water depth and effective gravity. At the microscopic scale, this is realized through the deployment of anisotropic arrays of vertical pillars and baffles that induce directional permeability, alongside periodic Helmholtz resonance cavities engineered for subwavelength wave trapping and targeted low-frequency attenuation.

At the macroscopic scale, these subwavelength designs culminate in the realization of ocean wave cloaking, including advanced invisibility and carpet cloaks, which present a transformative approach for the protection of aging coastal bridge piers and offshore platform structures. Rather than merely withstanding hydrodynamic loads, these metamaterial envelopes smoothly redirect incident wave energy around critical targets. This diversion establishes a centralized "calm water zone" that effectively eliminates direct hydrodynamic impact forces while simultaneously preventing severe bottom scouring and foundation erosion. Fig. X d1 details the engineered physical structures utilized for advanced water wave manipulation. The efficacy of these configurations is further demonstrated in Fig. X d2, where the schematic and simulated amplitude profiles of a water wave concentrator equipped with baffles reveal how incident wavefronts can be distinctly compressed and localized[32]. Furthermore, Fig. X d3 elucidates the functionality of an "invisibility concentrator" through comparative simulated field patterns[33]. It highlights that while an isolated large cylinder suffers from massive hydrodynamic scattering and severe wave run-up, the same cylinder enclosed by the metamaterial concentrator exhibits drastically suppressed scattering, facilitating a smoothly guided wave field that harmlessly bypasses the core structure.

This paradigm further inspires a fundamental departure from conventional coastal defense. Traditional concrete breakwaters rely on brute-force reflection, incurring high material cost and ecological disruption. In stark contrast, next-generation eco-friendly breakwaters integrate arrays of Helmholtz-resonator oscillating water columns, shifting the operational principle from hard resistance to intelligent, frequency-selective wave absorption and dissipation. Rather than merely blocking waves, these metastructures concentrate and trap the destructive energy, converting it into usable electricity through embedded piezohydraulic transducers or low-head turbines. The system thus simultaneously shelters coastlines, preserves marine ecosystems, and harvests clean energy, realizing in full the multi-physics empowerment that elevates structural metamaterials beyond their conventional load-bearing role.

1.	Pang, Y., et al., Triboelectric Nanogenerator-Enabled Digital Twins in Civil Engineering Infrastructure 4.0: A Comprehensive Review. Adv Sci (Weinh), 2024. 11(20): p. e2306574.

2.	Boafo, G. and D.K. Biswal, Advances in functional metamaterials: bridging mechanical, acoustic innovations with multifunctionality and adaptive responses. Results in Engineering, 2025. 28.

3.	Xu, G., T. Guo, and A.Q. Li, Rethinking structural safety for a volatile century. Fundam Res, 2026. 6(1): p. 335–337.

4.	Alavi, A.H., Metamaterials Break the Constraints of Traditional Civil Infrastructure. Advanced Materials, 2026. 38(6): p. e18198.

5.	Li, Z., et al., Emerging acousto-mechanical metamaterials: From physics-guided design to coupling-driven performance. Materials Today, 2025. 89: p. 151–171.

6.	Li, Z.-Y., et al., A self-sensing and self-actuating metamaterial sandwich structure for the low-frequency vibration mitigation and isolation. Composite Structures, 2022. 297: p. 115894.

7.	Zhang, X., Gene-modified acoustic metamaterials for improving the low-frequency broadband noise reduction performance of sound barriers for transportation buildings. 2025.

8.	Maldovan, M., Sound and heat revolutions in phononics. Nature, 2013. 503(7475): p. 209–217.

9.	Liu, Z., et al., Topological thermal transport. Nature Reviews Physics, 2024. 6(9): p. 554–565.

10.	Zhang, T., et al., Mechanical in-sensor computing: A programmable meta-sensor for structural damage classification without external electronic power. Mechanical Systems and Signal Processing, 2025. 240: p. 113347.

11.	Slabý, V., et al., Novel metamaterial platform with piezoelectric sensors for self-sensing mechanical support. International Journal of Mechanical Sciences, 2026. 314: p. 111387.

12.	Zhao, C., Bandgap mechanism and seismic wave attenuation performance of buried seismic metamaterials with double resonators. 2025.

13.	Xu, S., et al., Design of a broadband noise reduction barrier utilizing acoustic metamaterial with application to a substation. iScience, 2026. 29(6): p. 115918.

14.	Zhang, Y., et al., Foldable acoustic metamaterial for underwater broadband low-frequency noise mitigation. 2026.

15.	Feyisa, T., et al., Optimizing thermal radiation control with ultra-broadband metamaterials for high passive radiative cooling efficiency. Scientific Reports, 2025. 15(1): p. 43150.

16.	Li, Y., et al., Transforming heat transfer with thermal metamaterials and devices. Nature Reviews Materials, 2021. 6(6): p. 488–507.

17.	Farhangdoust, S., et al., Kirigami auxetic structure for high efficiency power harvesting in self-powered and wireless structural health monitoring systems. Smart Materials and Structures, 2021. 30(1): p. 015037.

18.	Shi, X., et al., Low-cost foam cementitious electromagnetic metamaterial with bioinspired periodic array structure. Composites Part B: Engineering, 2026. 324: p. 113843.

19.	Zhu, S., et al., Controlling water waves with artificial structures. Nature Reviews Physics, 2024. 6(4): p. 231–245.

20.	Saifullah, Y., et al., Metamaterials for Water Waves: Theory, Design, and Applications. Advanced Functional Materials, 2026. 36(28): p. e21623.

21.	Kryuchkyan, G.Y. and K.Z. Hatsagortsyan, Bragg scattering of light in vacuum structured by strong periodic fields. Phys Rev Lett, 2011. 107(5): p. 053604.

22.	Sugino, C., et al., A general theory for bandgap estimation in locally resonant metastructures. Journal of Sound and Vibration, 2017. 406: p. 104–123.

23.	Lupton, J.M., et al., Bragg scattering from periodically microstructured light emitting diodes. Applied Physics Letters, 2000. 77(21): p. 3340–3342.

24.	Fan, C.Z., Y. Gao, and J.P. Huang, Shaped graded materials with an apparent negative thermal conductivity. Applied Physics Letters, 2008. 92(25): p. 251907.

25.	Narayana, S. and Y. Sato, Heat Flux Manipulation with Engineered Thermal Materials. Physical Review Letters, 2012. 108(21): p. 214303.

26.	Li, Y., et al., Temperature-Dependent Transformation Thermotics: From Switchable Thermal Cloaks to Macroscopic Thermal Diodes. Phys Rev Lett, 2015. 115(19): p. 195503.

27.	Shen, Z., et al., The metamaterial sensors for multi-parameter measurement in structural health monitoring. Measurement, 2025. 245: p. 116652.

28.	Han, X., et al., A kirigami-metamaterial triboelectric nanogenerator for real-time wave load monitoring and early warning in marine structures. Measurement, 2026. 258: p. 119271.

29.	Li, W., et al., Triboelectric-electromagnetic metamaterial systems for self-powered multiparameter wireless monitoring. Nano Energy, 2026. 147: p. 111586.

30.	Park, J., J.R. Youn, and Y.S. Song, Hydrodynamic Metamaterial Cloak for Drag-Free Flow. Phys Rev Lett, 2019. 123(7): p. 074502.

31.	Zhang, Z., et al., Boundary effects of anisotropic medium on cloaking under shallow-water waves. Ocean Engineering, 2024. 291: p. 116485.

32.	Li, C., et al., Concentrators for Water Waves. Phys Rev Lett, 2018. 121(10): p. 104501.

33.	Invisibility concentrator for water waves. Physics of Fluids, 2020. 32(8).